ERASMUS+ - SECTOR SKILSS ALLIANCE

[DURATION: November 2014 – October 2017]

Unit of Learning Outcomes

# Composite Materials

[WORKPACKAGE 3: Designing joint curriculum]

[OUT 3.1 and 3.2: unit of learning outcomes]

PREPARED BY: P6-RTC and P4-MASOC in cooperation with P3-VISC

February 2016

1.	Description of short training programme

| Learning outcomes | The learners/trainees are able to: specify polymer, metal, ceramic composite materials according to their matrix and reinforcement component, compare composites with traditional materials; define markings of composite materials using manufacturers’ standards; choose composite materials and their processing way according to work task; choose processing tools using manufacturers’ catalogues; calculate processing parameters according to characteristics of materials, processing and geometry of the tools. |
| --- | --- |
| Relation to the national qualification/education NQF/EQF | SI: NQF 4/ SQF 5 LV: NQF/EQF 4 SK: NQF 3/SQF 4 HR: NQF 4.1, 4.2/EQF 4 |
| Links to existing educational programs | SI: Mechanical engineering technician Mechatronics engineering technician LV CNC operator Industrial mechanic Engineering technician Mechatronics system technician SK: Electrical engineering – electrical installations Electromechanician Mechanical engineering Mechanician – extender Toolmaker Mechanical production HR: Mechanical computer technician Mechatronics engineering technician Computer technician in mechanical engineering CNC operator 3 years |
| ECVET points | SI: 1 ECVET point LV: 1 ECVET point SK: 1 ECVET point HR: 1 ECVET point |
| Assessment criteria | Field of evaluation Evaluation criteria Points 1 Planning The candidate uses different sources of information, plans materials according to their characteristics and use, methods and tools he needs for the execution of work tasks. 40 2 Execution The candidate executes working tasks: define markings. The candidate is independent and innovative at his work and uses expertise he had acquired through training. 30 3 Documentation The candidate elaborates technical documentation and documentation of performance tasks. 10 4 Presentation The candidate systematically presents the individual stages of the construction of their tasks. 20 TOTAL 100 Pass criteria 60 |
| Work task (annex) | Examples. Include the documentation with information about exam (annex) |
| Forms and methods of work | Teaching/ learning forms: Frontal, pair work and group work, individual work - work with technical documentation, portfolio, ICT use, homework. Working methods: lectures – theoretical and practical topics presentation, practical exercises – solving some practical exercises during the class work, case study, problem solving, observation and detection, conversation, discussion, project work, using acquired skills and experience in a new situation, self-evaluation. |
| Material conditions for the training | The training provider must ensure: bright and airy space with working tables, a class equipped with multimedia, learning materials, PC with appropriate software, practical material samples or semi-finished parts for each topic, practical technological and calculation examples, technical documentation, handbooks, manufacturers' catalogues, e-catalogues. |
| Personal references | Training and examinations can be carried out by a person with required professional competences/ education and experience according to national regulations. |
| Framework curriculum (vocational school) | Legal bases for the education in vocational schools according to respective occupation. |
| Framework curriculum (in company) | Legal bases for the training in companies according to respective occupation. |

Annex: work tasks

| Learning outcomes | Work tasks |
| --- | --- |
| Specify polymer, metal, ceramic composite materials according to their matrix and reinforcement component, compare composites with traditional materials. | The candidate names : the main classification and characteristics of composite materials, physical characteristics (persistence, elasticity, viscosity), chemical characteristics (composition, structure – filled, reinforced, flaky). Explains classification principles according to matrix, filler. Characterizes composite materials with metallic matrix, composite materials based on non-metal and polymer materials. Explains the structure of composites: geometry, and placing of the structure elements. Compares the characteristics of composite materials with traditional materials. Describes and compares characteristics, production and use of different composite materials (metal-, polymer- and ceramic-). Classifies composite materials according to their matrix and filling stuff. Specifies 3 kinds of composite materials: metallic, non-metallic, polymer. Describes composites depending on their components (metallic, polymer, ceramic). |
| Define markings of composite materials using manufacturers’ standards | Reads different manufacturers’ standards. Explains the difference and use of manufacturers’ standards. Uses proper markings. |
| Choose composite materials and their processing way according to work task | Compares different composite materials. Selects appropriate composite materials according to the work task and names them. Clarifies the choice. |
| Choose processing tools using manufacturers’ catalogues | Works with multimedia: e-catalogues, uses the pixel code, downloads of catalogues and software. Chooses the suitable processing tools according to materials, names them and calculates machining parameters. Compares tools and makes the most rational and optimal choice taking into account prices, availability, supply. Selects the suitable tools according to the work piece materials and work task. |
| Calculate processing parameters according to characteristics of materials, processing and geometry of the tools | Calculates processing parameters according to characteristics of the composite material, geometry grade of the tool. Calculates cutting speed and machine speed, chooses of the cutting depth according to geometry of the tool. |

- Assessment:

| Learning outcomes | Skills and areas of knowledge should be tested | Methods | 1 Plan. | 2 Exe. | 3 Doc. | 4 Pre. |
| --- | --- | --- | --- | --- | --- | --- |
| Specify polymer, metal, ceramic composite materials according to their matrix and reinforcement component, compare composites with traditional materials. | Use theoretical and practical knowledge on the physical and chemical characteristics, production, processing and use of composite materials. Knowledge of all the reinforcement and matrix materials. | written test oral practical exercise | - | 15 | - | - |
| Define markings of composite materials using manufacturers’ standards | Understanding of the purpose of using manufacturers’ catalogues and other information materials to ensure the correct result in specification of the material. | written test oral test | 15 | - | - | - |
| Choose processing way of composite materials according to work task | Knowledge of types of the tools and processing parameters for the material. | practical exercise reporting | 5 | 10 | 10 | - |
| Choose processing tools using manufacturers’ catalogues | Ability to select the correct tool for the processing operation | reporting demonstration discussion | 15 | - | - | 10 |
| Calculate processing parameters according to characteristics of materials, processing and geometry of the tools | Ability to define the material grade and set the machining parameters according to the necessary processing operation. | practical exercise | 5 | 5 | - | 10 |
| SUM |  |  | 40 | 15 | 10 | 20 |

3. Process/execution method:

| Information and Planning | The candidate is familiar with the objectives of the tasks. He plans work process using technical information, drawings, descriptions, tables, charts, manufacturers’ standards. The candidate uses different sources of information in devising. The candidate plans materials, methods and tools he needs for the execution of tasks. The candidate prepares working documents ( standards, tables. |
| --- | --- |
| Execution of Work | The candidate is independent and original in his work. The candidate correctly uses manufacturer’s standards. The candidate chooses materials, marks them. The candidate chooses the suitable cutting tools and to calculate machining parameters. The candidate works with multimedia: e-catalogues, uses the pixel code, downloads of catalogues and software. The candidate calculates processing parameters taking into account workpiece materials. The candidate calculates cutting speed and machine speed, chooses of the cutting depth according to geometry of the tool. The candidate works with manufacturers’ catalogues: defining processing parameters and tool life choose of appropriate instruments and tools. The candidate defines the physical and chemical characteristics of composite materials. The candidate classifies composites, produces and uses them. In the task execution, the candidate uses expertise he had acquired through education. |
| Control and Evaluation | The candidate evaluates the quality of the work, corrects errors if it is necessary. |
| Cleaning and Waste Disposal | The candidate arranges the work place after completing the work. He separates and appropriately, stores waste materials. |
| Work Safety and Health Protection | The candidate observes safety regulations of the company and health protection regulations; takes remedial action in case of hazard potentials. |
| Work Attitude | The candidate works carefully and responsibly, communicates adequately shows commitment. |